**Purchase Specifications for a**

**24 Inch Barrier Float (also known as a Line Float, Buoy Line)**

Sealite SL-BF-2436

**Overview**

This specification is for a 24 inch diameter by 36 inch long marine float (also known as a barrier

float, line float, buoy line).

Each float shall be made from UV inhibited polyethylene low linear density polyethylene (LLEDPE) in International Orange color as standard with other color options available

Each float shall be rotationally molded as a single piece.

Each float shall be filled with closed cell polyurethane foam.

**1.0 Float Characteristics**

Each float shall have a total volume of 56.5 gallons (214 litres)

Each float shall have a total reserve buoyancy of 370 lbs. (168 kg)

Each float shall have a wall thickness of .2 inch (5 mm)

Each float shall have a length of 36 inches (914 mm)

Each float shall have a diameter of 24 inches (610 mm)

Each float shall weigh 39 lbs. (17.5 kg)

**2.0 Material Characteristics**

Each float shall be manufactured as a single piece using a rotational molded process.

Each float shall have an outer shell made from low linear density polyethylene (LLEPE) with ultra-violet

(UV) inhibition properties.

Each float shall be filled with closed cell polyurethane foam.

Each float shall be made without toxic chemicals or heavy metals.

Each float shall be impact resistant.

**3.0 Options**

Each float shall be offered in the following oval styles available from the manufacturer:

• 1.5 inch (128 mm) diameter HDPE pipe thru float which is molded in place at time of

production (known as Sealite part number SL-BF2436)

• 1/2 inch diameter galvanized steel rod thru the middle with ½ inch swivels (also known as

thimbles) at both ends (known as Sealite part number SL-BF2436-S)

Each float shall be available in the alternative colors of red, green and yellow.

ID labels and custom graphics shall be available as options.

**4.0 Environmental Factors**

Each float shall have an outer shell made from LLDPE that does not use toxic chemicals or heavy metals in the

manufacturing process.

Each float shall be recyclable.

**5.0 Certifications**

Each float shall be produced by a certified ISO 9001:2015 manufacturer.

Each float shall offer USCG compliant options.

Each float shall contain closed cell polyurethane foam that meets 33 CFR 183.114.

6.0 **Warranty**

Each float shall have a one (1) year warranty.

Purchase Specifications SL-BF-2436-V1